## Slide 1
Eggshell–Agar
Biocomposites
Development and characterisation for sustainable interior applications
Betül Ünal
Department of Interior Architecture
Cappadocia University
ICSMMEP-26 · MECCA · 3–4 NOVEMBER 2026
Notes: Good morning. Betul Unal, Department of Interior Architecture, Cappadocia University. The panel in the photograph is the subject of this paper: a composite of waste eggshell bound in agar, cast at 300 by 300 millimetres. Over the next fifteen minutes I will set out the production protocol, the characterisation results, and an argument about how materials of this class should be evaluated.

## Slide 2
Background
Point of departure
Eggshell arises continuously as a food-processing by-product and is predominantly landfilled. It accounts for roughly a tenth of the mass of every egg, so the stream is neither small nor intermittent. Chemically it is almost pure calcium carbonate held in a porous, protein-bound crystalline structure, with a specific gravity below that of most mineral fillers used in construction.
Its composition and its uninterrupted supply have made it an established secondary mineral resource, and a substantial body of work has incorporated it into construction and polymer materials.
William & Owen (1995) · Torres et al. (2010) · Owuamanam & Cree (2020)
Material basis
94–97%
calcium carbonate by mass
0.85–2.66
specific gravity, below most mineral fillers
> 12
months of single-source collection for this study
Disposal and valorisation routes
Food processing
Waste eggshell
Landfill — current practice
Secondary mineral resource
The case for eggshell as a mineral phase is settled. This paper is concerned with the phase that binds it.
Notes: The point of departure. Eggshell arises continuously as a food-processing by-product and is predominantly landfilled. Chemically it is almost pure calcium carbonate, between ninety-four and ninety-seven percent by mass, held in a porous protein-bound crystalline structure, and its specific gravity sits below that of most mineral fillers used in construction. That composition and that uninterrupted supply are why a substantial literature already incorporates it into construction and polymer materials. All shell used in this study came from a single bakery, collected over more than a year. I want to be clear at the outset: the case for eggshell as a mineral phase is settled, and this paper does not re-make it. The paper is concerned with the phase that binds it.

## Slide 3
Prior applications
Established uses of eggshell waste in engineered materials
Application | Binding phase | Reference
Partial cement replacement in concrete | Portland clinker | Teara et al. (2019); Bhartiya & Dubey (2018)
Compressed laterite brick | Soil – lime | Adogla et al. (2016)
Hot-mix asphalt | Bitumen | Razzaq & Yousif (2017)
Clay stabilisation | Clay mineral | Soundara & Vilasini (2015)
Eco-ceramic wall tile | Ceramic body | Vilarinho et al. (2022)
Particulate filler in PVC | Poly(vinyl chloride) | Skórczewska et al. (2020)
Filler in flexible polyurethane foam | Polyurethane | Victor et al. (2019)
Ceramic–metal composite | Metal matrix | Bilici et al. (2023); Yönetken et al. (2016)
Bone tissue scaffold | Calcium phosphate | Shafiei et al. (2019)
Wallpaper | Cellulosic furnish | Tutuş et al. (2018)
What every row above has in common
MINERAL PHASE · recovered from waste in every study above
BINDING PHASE · cementitious, ceramic or petrochemical in every study above
Notes: This is the literature the study departs from, and reading down the middle column is the whole argument. Eggshell has been used as a partial cement replacement in concrete, as a stabiliser in compressed laterite brick and in clay, as a filler in hot-mix asphalt, in eco-ceramic wall tile, as a particulate filler in PVC and in flexible polyurethane foam, in ceramic-metal composites, in bone scaffolds, and even in wallpaper. The valorisation is real and it is well evidenced. But in every one of those cases the mineral is recovered from waste while the binding phase remains cementitious, ceramic or petrochemical. The environmental burden of the material is carried by the binder, and the binder is untouched.

## Slide 4
Agar as binder
Properties and existing characterisation
Agar is a thermoreversible polysaccharide extracted from red seaweed. It melts on heating and sets on cooling without chemical crosslinking, so no reactive hardener is required. Its behaviour with glycerol has been mapped systematically across 32 formulations and released as an open reference dataset.
Scope of that characterisation
Unfilled thin films, loaded in uniaxial tension, evaluated for packaging. Agar has not been characterised as the binding phase of a mineral-filled cast solid in bending.
Thermoreversible setting
Gel — solid
Sol — in solution
heat, 95 °C
cool, ambient
The transition is physical, not chemical: no reactive hardener, no cure temperature, and at 66% mineral loading no coupling agent.
Form and loading case in this study
— | Film literature | This study
Form | Thin cast film | Cast solid, 20–50 mm
Mineral phase | Unfilled | 66% of solids
Loading | Uniaxial tension | Compression and bending
Intended use | Packaging | Interior surfaces
The compositional logic transfers. The form and the loading case do not, and it is the loading case that governs use as an interior surface.
Hernández et al. (2022), Materials 15(11), 3954 — 32 agar / glycerin / water formulations, released as an open dataset.
Notes: The binder is agar, a thermoreversible polysaccharide extracted from red seaweed. It melts on heating and sets on cooling without chemical crosslinking, which means no reactive hardener and no elevated-temperature cure. Its behaviour with glycerol is reasonably well mapped: Hernandez and colleagues ran thirty-two agar, glycerin and water formulations by design of experiments in 2022 and released the dataset openly. But note the scope of that work. Unfilled thin films, loaded in uniaxial tension, evaluated for packaging. The compositional logic transfers to this study. The form and the loading case do not, and for an interior surface the loading case is bending.

## Slide 5
Research gap
Three gaps follow from the preceding two slides
01
The binding phase is never biological
Across the eggshell literature the mineral is recovered from waste while the matrix remains Portland clinker, bitumen, lime, a ceramic body or a thermoplastic. No study reports an eggshell composite in which both phases are of biological origin and fully biodegradable.
02
Agar is characterised only as an unfilled film
The reference dataset covers thin films in uniaxial tension for packaging. The behaviour of agar as the binding phase of a highly mineral-filled cast solid, loaded in bending, is not reported.
03
Property sets are reported in fragments
Compressive, flexural, reaction-to-fire and hygric behaviour are reported in separate studies on separate formulations. No single study gives all four for one eggshell–biopolymer formulation family.
The contribution is therefore a documented protocol and a single coherent property set, not a novel constituent.
Notes: Three gaps follow directly from those two slides. First, the binding phase is never biological. Across the whole eggshell literature the mineral is recovered from waste while the matrix stays Portland clinker, bitumen, lime, a ceramic body or a thermoplastic - no study reports an eggshell composite in which both phases are biological and fully biodegradable. Second, agar is characterised only as an unfilled film in tension for packaging, not as the binder of a highly mineral-filled cast solid in bending. Third, property sets are reported in fragments: compressive, flexural, fire and hygric behaviour appear in separate studies on separate formulations, and no single study gives all four for one formulation family. I want to state the contribution precisely, because overclaiming here would be easy. It is not a novel constituent. It is a documented protocol and a single coherent property set.

## Slide 6
Aim
To document a reproducible production protocol for a fully bio-based eggshell–agar composite, and to characterise its mechanical, reaction-to-fire and hygric behaviour against published test standards.
Objectives
01
Document the protocol in full
Every parameter of mineral preparation, binder preparation, casting and cure reported in a form another laboratory can repeat.
02
Characterise against published standards
Compressive and flexural behaviour, ignitability and water absorption, determined to ASTM D790-17, ISO 11925-2:2020 and ASTM D570-98.
03
Position the results
Benchmarked against conventional interior materials and against the bio-based composite family, from published property data.
04
Derive an evaluation criterion
Establish which measured quantity governs service behaviour for this material class, and report it alongside strength.
Notes: The aim, stated narrowly on purpose: document a reproducible production protocol for a fully bio-based eggshell-agar composite, and characterise its mechanical, reaction-to-fire and hygric behaviour against published test standards. Four objectives follow. One, document the protocol in full, every parameter, in a form another laboratory can repeat. Two, characterise against published standards rather than ad hoc procedures. Three, position the results against two material families using published property data. Four, derive an evaluation criterion appropriate to this material class - and that fourth objective is the one I will spend most time on at the end.

## Slide 7
Scope
Within scope
Dimension | This study
Formulations | Five — three compressive, two flexural
Specimens | Three per formulation for mechanical testing
Properties | Compression, flexure, ignitability, water absorption, bulk density
Standards | ASTM D790-17 · ISO 11925-2:2020 · ASTM D570-98(2018)
Conditions | Ambient cure, single laboratory, single operator
Application | Non-loadbearing interior surfaces
Outside scope
No durability, classification or life-cycle data were generated. The results reported here are characterisation data, not a performance specification.
Each exclusion is revisited as a defined next experiment in the closing section.
Property coverage
Compression
Flexure
Ignitability
Water absorption
Bulk density
Durability
Fire classification
Life-cycle
Structural use
Filled: determined in this study. Outlined: not determined, and therefore outside every claim made in this presentation.
Notes: Scope, set out explicitly so that nothing I say today is read beyond it. Within scope: five formulations, three specimens per formulation for the mechanical work, five properties, three published standards, ambient cure in a single laboratory by a single operator, and an application envelope of non-loadbearing interior surfaces. Outside scope: structural use, durability and accelerated ageing, reaction-to-fire classification, and life-cycle assessment. None of those four was generated in this work. What follows is characterisation data, not a performance specification, and I will return to each exclusion at the end as a defined next experiment.

## Slide 8
Method
A material-driven sequence in four stages
1
Produce
Develop the composite and record every production parameter.
Iterative formulation over twelve months
2
Measure
Characterise the cured material against published test standards.
Compression · flexure · ignitability · absorption
3
Position
Benchmark the results against two material families.
Conventional interior materials · bio-based composites
4
Propose
Derive an evaluation criterion from the observed behaviour.
Deformation capacity reported alongside strength
The order is material-driven: properties are measured first and the application envelope is derived from them, rather than the material being selected to satisfy a predetermined form. The design proposal presented later follows from the measurements and not the reverse.
Material-driven design after Karana et al. (2015)
Notes: Four stages, and the order is the method. Produce, recording every production parameter. Measure against published standards. Position against two material families, conventional interior materials and bio-based composites. And propose an evaluation criterion derived from the observed behaviour. This is a material-driven sequence in the sense of Karana and colleagues: the properties are measured first and the application envelope is derived from them, rather than the material being selected to satisfy a form decided in advance. The design proposal I show near the end follows from the measurements and not the reverse.

## Slide 9
Research questions
01
Which formulation variable governs compressive strength?
Formulation
02
How does plasticiser content affect flexural behaviour?
Formulation
03
How does the composite compare with conventional interior materials?
Benchmark
04
How does it compare with other bio-based composites?
Benchmark
05
Is compressive strength an adequate evaluation criterion for this class?
Criterion
Questions one to four are answered by measurement. Question five is answered by argument from those measurements.
Notes: Five research questions. The first two are formulation questions - which variable governs compressive strength, and what plasticiser content does to flexural behaviour. The next two are benchmarking questions against the two material families. The fifth asks whether compressive strength is an adequate evaluation criterion for this class of material at all, and it is the question I care most about. Questions one to four are answered by measurement. Question five is answered by argument from those measurements, which is a different kind of claim and I will flag it as such when I get there.

## Slide 10
Hypothesis
A fully bio-based eggshell–agar composite can be produced repeatably under ambient conditions, and its performance as an interior surface material is governed by deformation capacity rather than by compressive strength.
Two clauses, tested separately
Clause 1
Producible repeatably under ambient conditions
Tested by the production protocol and the formulation series: a defined procedure, a fixed shell-to-binder ratio, five formulations and a cure requiring no thermal input after mixing.
Slides
12–15
Clause 2
Governed by deformation capacity rather than strength
Tested by the mechanical results and the two benchmarks: the failure mode in compression, the flexural response, and the position of the modulus of resilience relative to strength.
Slides
17–24
Provenance. The dissertation from which this work derives states a broader hypothesis framed on spatial resilience in interior design. The formulation above is the materials-engineering component of it, restated within the scope of the tests reported here.
Notes: The hypothesis, in two clauses, because the two are tested by different parts of the paper. First clause: a fully bio-based eggshell-agar composite can be produced repeatably under ambient conditions. That is tested by the protocol and the formulation series - a defined procedure, a fixed shell-to-binder ratio, five formulations, and a cure that requires no thermal input after mixing. Second clause: its performance as an interior surface material is governed by deformation capacity rather than by compressive strength. That is tested by the mechanical results and the two benchmarks. On provenance, and I would rather say this than have it asked: the dissertation this derives from states a broader hypothesis framed on spatial resilience in interior design. What you see here is the materials-engineering component of that, restated within the scope of the tests actually reported.

## Slide 11
Four constituents, each biodegradable
Waste eggshell powder · agar · glycerol · water, with a shellac finish. Colour and texture vary with natural pigment and mould geometry at constant composition.
Notes: The material. Four constituents: waste eggshell powder as the mineral phase, agar as the binder, glycerol as the plasticiser, water as the carrier, with a shellac finish where water resistance is required. Everything in this photograph is one formulation family - the variation in colour and texture comes from natural pigment and mould geometry, not from different compositions. The dark tones are beetroot.

## Slide 12
Stage 1 · Mineral phase
Progressive size reduction of the shell to a sieved powder
Whole shell
collected from a single bakery
—
Cleaned
membrane and residue removed manually
—
Heat-treated
decontamination and drying
120 °C, 20 min
Milled
laboratory mechanical grinder
to homogeneous powder
Sieved
passing fraction retained
150 µm mesh
Particle size rationale
The 150 µm fraction was selected to match the particle size used in the eggshell polymer-composite literature, so that the mineral phase in this study is comparable with that body of work.
Terminology
The 120 °C step is reported as decontamination and drying, not sterilisation. Dry-heat sterilisation requires substantially higher temperatures for longer, and sterility was not verified.
Notes: Stage one, the mineral phase. Whole shell from a single bakery, cleaned of membrane and residue by hand, heat-treated at 120 degrees for twenty minutes, milled in a laboratory grinder to a homogeneous powder, and sieved through a 150 micrometre mesh with only the passing fraction retained. The circles contract across the diagram to show what the stage actually does, which is progressive size reduction. Two points of precision. The 150 micrometre figure was selected to match the particle size used in the eggshell polymer-composite literature, so that the mineral phase here is comparable with that work. And I report the 120 degree step as decontamination and drying rather than sterilisation, because dry-heat sterilisation requires around 160 to 170 degrees for one to two hours and sterility was not verified.

## Slide 13
Stage 2 · Binder preparation
Temperature–time profile of the 55-minute preparation
95 °C
80 °C
ambient
55 min total
Water and glycerol
pre-mixed, no solids present
Agar dissolution
added incrementally, stirred
Viscosity development
continuous stirring
Shell addition
incremental, near the end
Agar is taken into solution before viscosity develops; incremental addition prevents agglomeration, and the shell fraction is introduced late to prevent sedimentation.
Schematic. The two set points and the total heating time are recorded; intermediate ramp rates are not, and are drawn indicatively. Stirring was manual, so shear rate is not a controlled quantity.
Notes: Stage two, binder preparation, drawn as a temperature-time profile because that is what the stage is. Water and glycerol are pre-mixed first, before any solids are present. Agar is then added incrementally under continuous stirring - bulk addition forms agglomerates that do not redisperse. The mixture is taken to 95 degrees and held until the agar is fully in solution, because if viscosity builds before complete dissolution the gel network is patchy. The temperature is then reduced to 80 and held while viscosity develops, and the shell fraction is introduced incrementally near the end; introduced earlier, it sediments. Fifty-five minutes in total. This is a schematic: the two set points and the total time are recorded, the intermediate ramp rates are not, and stirring was manual so shear rate is not a controlled quantity.

## Slide 14
Stage 3 · Casting and cure
Eleven days from casting to finished specimen, without thermal input
In mould
setting and initial drying
Ambient consolidation
≈ 23 °C, shielded from direct sun and air movement
Day 0
cast into silicone moulds
Day 4
demoulded
Day 11
finished specimen, three shellac coats
Mould material
Silicone, flexible enough to release without a parting agent and without damaging a partially consolidated specimen. 50 mm cube moulds for compression, flat moulds otherwise.
Thermal input
None after the 55-minute preparation. The entire cure proceeds at room temperature, which is relevant to the embodied-energy argument.
Limitation the composite shrinks appreciably as water evaporates. Cross-sections were measured at test time, but post-drying dimensions were not logged, so every dimension quoted in this presentation is a mould dimension.
Notes: Stage three, casting and cure, drawn as a timeline. Day zero, cast into silicone moulds - silicone because it flexes enough to release without a parting agent and without damaging a specimen that has not fully consolidated. Four days in mould for setting and initial drying, demoulded on day four, then seven further days at around 23 degrees shielded from direct sun and forced air movement. Day eleven, finished specimen, with three shellac coats where water resistance is required. Note that there is no thermal input at all after the fifty-five minute preparation: the entire cure proceeds at room temperature, which matters for the embodied-energy argument later. The limitation, which I will repeat because it affects every number that follows: the composite shrinks appreciably as water evaporates, cross-sections were measured at test time but post-drying dimensions were not logged, so every dimension I quote is a mould dimension.

## Slide 15
Formulations
Five mixes, with the derived ratios that govern the results
ID | Test | Water g | Shell g | Agar g | Glycerol g | Solids g | Shell : binder | Solids : water | Glycerol % solids
C1 | Compression | 325 | 80 | 35 | 5 | 120 | 2.00 | 0.37 | 4.2
C2 | Compression | 310 | 90 | 40 | 5 | 135 | 2.00 | 0.44 | 3.7
C3 | Compression | 280 | 110 | 45 | 10 | 165 | 2.00 | 0.59 | 6.1
F1 | Flexure | 450 | 190 | 70 | 60 | 320 | 1.46 | 0.71 | 18.8
F2 | Flexure | 480 | 190 | 70 | 30 | 290 | 1.90 | 0.60 | 10.3
Batch composition by mass
water
shell
agar
glycerol
C1
73% water
C2
70% water
C3
63% water
F1
58% water
F2
62% water
Compressive series
Shell-to-binder is held at exactly 2.00 across all three mixes, so solids concentration is the only variable — the water band shortens from C1 to C3.
Flexural series
Glycerol was halved at fixed batch mass, so water rose with it. The plasticiser effect is not isolated.
Three specimens per formulation. Values reported later are means; individual values were not retained, so standard deviations cannot be given.
Notes: The formulation matrix with the derived ratios, and there are two things to read in it. In the compressive series shell-to-binder is exactly two point zero zero in all three mixes. That was not planned as a control, but the consequence is that solids concentration is the only variable in the series, which makes the compression result interpretable. In the flexural series I declare a confound: glycerol was halved but batch mass was held at 770 grams, so water rose to compensate and the other ratios shifted with it. The plasticiser effect is therefore not cleanly isolated, and I will say so again when I present the flexural data.

## Slide 16
Test programme
Five properties, three published standards, four specimen geometries
Property | Standard | n | Quantity measured
Compressive behaviour | Cube compression | 3 per mix | Maximum load; compressive stress
Flexural behaviour | ASTM D790-17 | 3 per mix | Flexural strength; flexural modulus
Reaction to fire | ISO 11925-2:2020 | 2 | Time to ignition; time to extinguish
Water absorption | ASTM D570-98(2018) | 1 | Mass gain over 24 h immersion
Bulk density | Gravimetric | 1 | Mass per mould volume
Mechanical values are means of three specimens; individual values were not retained, so standard deviations cannot be reported. Ignitability, absorption and density rest on single determinations and are indicative rather than characteristic values.
Cube compression
50 mm cube, platen-loaded
Three-point flexure
180 × 60 × 20 mm, 120 mm span
Edge ignition
40 × 50 mm at 45°, 15 s flame
Immersion
40 × 50 mm, shellac-coated, 24 h
120 mm
45°
All testing: Advanced Construction Materials Research Laboratory, Hacettepe University. · Schematic, not to scale.
Notes: The test programme. I want the reporting convention on the record before any numbers appear. Mechanical values are means of three specimens; individual values were not retained, so I cannot give standard deviations. The ignitability, absorption and density figures rest on single determinations and are indicative rather than characteristic values. Compression was run as cube compression rather than to a named standard, and I flag that as a deviation.

## Slide 17
Compression
Measured values
ID | Solids : water | Fₘₐₓ kN | σᴄ MPa
C1 | 0.37 | 3.89 | 2.55
C2 | 0.44 | 4.30 | 3.12
C3 | 0.59 | 6.80 | 4.10
Compressive strength rises with solids concentration, not with mineral content.
Shell-to-binder is fixed at 2.00 across the series, so packing density is the only variable. The relation is linear over the range tested, R² = 0.99 — three formulations, and therefore a hypothesis rather than a law.
Fitted relation: σᴄ = 6.93 (solids : water) + 0.04
Chart: Compressive stress (MPa)
| C1 0.37 | C2 0.44 | C3 0.59
σ | 2.55 | 3.12 | 4.1
Solids : water ratio shown beneath each formulation identifier.
Notes: The compression result, and this answers research question one. Because shell-to-binder is fixed at two point zero zero across the series, solids concentration is the only variable - and compressive stress rises linearly with it, R-squared of 0.99 over the range 0.37 to 0.59. Three points will fit almost any line, so I am calling this a hypothesis rather than a law. But it has a clear physical reading: strength here is governed by packing density, not by mineral content as such. If that is right, the route to a stronger composite is to remove water rather than to add shell. The fitted relation is sigma equals 6.93 times the solids-to-water ratio plus 0.04.

## Slide 18
Compressive failure
Compressive stress (MPa) – strain, C3
Observed response
Linear to approximately 1 MPa, then progressive loss of stiffness
Peak stress near 10% strain, with no abrupt load drop
Continued deformation beyond peak with retained integrity
Interpretation
The agar network yields and the mineral redistributes rather than the section parting. Energy is absorbed rather than released, and the specimen remains a single body after test.
Failure proceeds by progressive crushing rather than by fracture.
For a demountable component this is the behaviour that governs service life: damage accumulates visibly rather than arriving as sudden loss of the section.
Strain derived from an assumed 10% maximum deformation based on observation, not instrumented measurement. · Bulk density 1.38 g/cm³, mould-volume basis.
Notes: This is the failure mode, and it is what I would ask about from where you are sitting. The curve is linear to about one megapascal, then stiffness falls away progressively as the agar network yields and the mineral redistributes. Peak arrives near ten percent strain with no abrupt load drop, and beyond peak the specimen continues to deform while holding together. The photograph shows the consequence: the cube has barrelled, it is shorter and wider, and it is still a single body. Energy is absorbed rather than released. One honesty point on the axis: the strain scale derives from an assumed ten percent maximum deformation based on observation, not from instrumented measurement.

## Slide 19
Flexure
Measured values — ASTM D790-17, three-point
ID | Glycerol % solids | Fₘₐₓ N | σꜰ MPa | Eꜰ MPa | ε peak
F1 | 18.8 | — | not measurable | — | —
F2 | 10.3 | 310 | 2.325 | 192 | 0.0121
Flexural stress (MPa) – strain, F2
At 18.8% glycerol the instrument registered no usable resistance. Halving the plasticiser gave a section that resists while still deforming substantially.
The transition lies between these two values.
Limitation
The specimen is kerfed on its tension face. The standard assumes a solid rectangular section and the calculation uses the full section, so part of the measured compliance is geometric and the reported modulus is a lower bound.
Flexural resistance is governed by plasticiser content.
The composition at which the composite ceases to resist and merely deforms lies between 10.3 and 18.8% glycerol on solids. Locating it is the first task of the next formulation series.
Confounded with solids concentration: batch mass was held constant, so water rose as glycerol fell.
Flexural strength computed as σꜰ = 3FL / 2bd² on the full rectangular section.
Notes: Flexure, to ASTM D790. The decisive variable is plasticiser content. At 18.8 percent glycerol the composite deformed without developing measurable resistance - the instrument registered nothing usable at all. Halving it gives 2.325 megapascals at a modulus of 192. The transition is sharp and it lies between those two values, which is itself a useful thing to know and a target for the next formulation series. Two limitations. The glycerol effect is confounded with solids concentration, as I flagged on the formulation slide. And the specimen is kerfed on its tension face while the standard assumes a solid rectangle, so the modulus I am quoting is a lower bound on the bulk material rather than a material constant.

## Slide 20
Flexural deformation
The beam is deflected well beyond the failure point of a comparable ceramic without parting. Transverse kerfs on the tension face permit the panel to be arched by hand.
The kerfs are also why the measured compliance is partly geometric, and why the reported modulus is a lower bound rather than a material constant.
Substantial deformation with retained integrity, in both test programmes.
Three-point rig at high deflection · close-up of the kerfed tension face · panel arched by hand
Notes: I would rather show this than ask you to take it on the numbers. On the left, the three-point rig at high deflection: the beam is deflected well past the failure point of a comparable ceramic and it has not parted. In the middle, a close-up of the tension face, where the transverse kerfs are visible. Below, the same panel arched by hand. The kerfs are why it arches, and they are also why I report the modulus as a lower bound rather than a material constant. The common result across both test programmes is substantial deformation with retained integrity, and that is the observation the final argument rests on.

## Slide 21
Fire, water, density
Ignitability
≈ 10 s
to ignition under direct flame
4 s
to self-extinguish after flame removal
Charring remains local
No lateral flame spread
No melting and no dripping
The probable mechanism is endothermic decomposition of the carbonate fraction, diluting the flame front. This was not verified calorimetrically.
ISO 11925-2:2020. Ignitability only: no Euroclass classification, cone calorimetry, smoke or toxicity data.
Water absorption, 24 h immersion
0.7%
mass gain, shellac-coated. Coating integrity rather than the composite is the limiting factor for humid service.
Bulk density
Material | g/cm³ | Reference
This study (C3) | 1.38 | —
Mycelium, cellulose | 0.3 – 0.8 | Jones et al. (2020)
Fired clay brick | 1.6 – 2.0 | William & Owen (1995)
Normal-weight concrete | 2.4 | William & Owen (1995)
Denser than the fungal and cellulosic family, lighter than fired clay. Mould-volume basis, therefore a lower bound.
Notes: Fire, water and density together. On ignitability: ignition at around ten seconds under direct flame, self-extinguishing four seconds after the flame is removed, with charring confined locally, no lateral spread, and no melting or dripping - which matters for a polymer-adjacent material. The probable mechanism is endothermic decomposition of the carbonate fraction releasing carbon dioxide and diluting the flame front, and I state that as a probable mechanism because it was not verified calorimetrically. To be precise: this is an ignitability test. There is no Euroclass classification, no cone calorimetry, no smoke or toxicity data. On water: 0.7 percent mass gain over twenty-four hours of full immersion with three shellac coats, with local dissolution where the coating was thin, so coating integrity is the limiting factor. On density: 1.38, above the fungal and cellulosic bio-materials and below fired clay, on a mould-volume basis and therefore a lower bound.

## Slide 22
Conventional materials
Compressive and flexural strength against interior surface materials
Chart: Strength (MPa)
| Compressed mushroom panel | This study (C3) | WPC | MDF | Travertine
Compressive | 1.2 | 4.1 | 7.2 | 24 | 80
Flexural | 1 | 2.3 | 12 | 35 | 11
Velasco & Gaona (2011) · Klyosov (2007) · Nemli & Aydın (2007) · Altun (2006)
Position
One sixth the compressive strength of MDF and one twentieth that of travertine, a stone the material visually resembles. Three times the compressive strength of compressed mushroom panel, the only other fully bio-based board in the set.
On strength alone the composite is not competitive with engineered wood or stone.
Notes: First benchmark, against the materials this would sit alongside in an interior. Let me be direct. One sixth the compressive strength of MDF and one twentieth that of travertine - and travertine is the relevant aesthetic comparison, because the material resembles it. It does exceed compressed mushroom panel, the only other fully bio-based board in the set, by a factor of three in compression. But on strength alone the composite is not competitive with engineered wood or stone, and I am not going to claim otherwise.

## Slide 23
Bio-based composites
Compressive strength
Material | σᴄ MPa | Reference
This study (C3) | 4.1 | —
Mycelium composite | 0.145 – 0.452 | Jones et al. (2020)
Hempcrete | 0.3 – 0.6 | Arnaud & Gourlay (2012)
Eggshell-filled PLA | 2 – 5 | Kim & Pal (2010)
Mineral-filled biocomposite | 2.1 – 39.6 | Shah et al. (2016)
Elastic modulus
Material | E MPa | Reference
This study (F2) | 192 | —
Mycelium composite | 1.8 – 5 | Islam et al. (2018)
Soy-based bioplastic | 124 | Mansour et al. (2021)
Flax-fibre PLA | 198 | Faruk et al. (2012)
LDPE | 100 – 300 | Zhao et al. (2022)
Wood (pine) | 11 000 | Pope & Hudson (1989)
Elastic modulus on a logarithmic scale, MPa
1
10
100
1,000
10,000
Mycelium
LDPE
Pine
This study 192
Water-cast and ambient-dried, the composite attains the stiffness range of melt-processed bio-polymers.
Unlabelled points: soy-based bioplastic 124 MPa, flax-fibre PLA 198 MPa. · An order of magnitude above the fungal and lime-binder family in compression; wood remains two orders of magnitude above in modulus. Values are reported as published; specimen geometry and test method differ between sources.
Notes: Second benchmark, and this is the one that matters. Against the bio-based family the position changes completely. In compression, an order of magnitude above mycelium composites and hempcrete, and within the range reported for eggshell-filled PLA. In stiffness, 192 megapascals - between soy bioplastic at 124 and flax-fibre PLA at 198, inside the LDPE range. Note what that means in process terms. This is water-cast and dried at room temperature, with no oven, no autoclave and no extruder, and it reaches the stiffness of melt-processed bio-polymers. One caution: the cited values come from studies with differing specimen geometry and test method, so this is a position statement rather than a controlled comparison. And wood remains two orders of magnitude above in modulus.

## Slide 24
Modulus of resilience
Elastic energy absorbed per unit volume
stress
strain
Ur
The shaded area is the energy absorbed per unit volume before permanent damage: ½ σ ε, and with ε = σ / E it reduces to the expression at right.
Ur = σ² / 2E
14.1 kJ/m³
computed from this study's own σꜰ = 2.325 MPa and Eꜰ = 192 MPa
Elastic modulus appears in the denominator.
The low modulus that counted against the material on the preceding slide is the same property that raises this quantity. Strength records the load at which performance ceases; it does not record whether failure is graceful or catastrophic.
Limitation
A comparative table cannot yet be assembled: the literature reports strength and modulus in separate studies on separate formulations.
This is a data point and a proposed reporting convention, not a ranking, and the value inherits the lower-bound modulus.
Resilience as a property of systems that absorb disturbance and retain function, after Holling (1973).
Notes: This brings me to research question five, and the diagram is the argument. The shaded area under the elastic region is the energy a material absorbs per unit volume before it takes permanent damage. Because that area is one half sigma epsilon, and epsilon is sigma over E, the area reduces to sigma squared over two E. Notice where the elastic modulus sits: in the denominator. So the low modulus that counted against the material on the previous slide is the same property that raises this quantity. For this formulation it comes to about 14 kilojoules per cubic metre, computed from this study's own two measurements. Both test programmes gave the same qualitative result, substantial deformation with retained integrity. Strength records the load at which a material ceases to perform. It does not record whether it then fails gracefully or catastrophically, and for a demountable non-loadbearing component that is what governs service life. The limitation, stated plainly: I cannot give you a comparative table, because the literature reports strength and modulus in separate studies on separate formulations. This is a data point and a proposed reporting convention, not a ranking, and the value inherits the lower-bound modulus.

## Slide 25
Application envelope
Modular proposal derived from the measurements
Demountable modules on a reversible fixing, replaceable one unit at a time.
Conditions of use, each traced to a measured result
Non-loadbearing surfaces
self-weight and handling loads only; σᴄ = 4.1 MPa
Dry interiors
not wet rooms, not façades; absorption depends on coating integrity
Away from ignition sources
self-extinguishing, but unclassified for reaction to fire
Modular rather than sheet
damage is replaced one unit at a time
End-of-life pathway
Every constituent, the shellac finish included, is biodegradable; reversible fixing allows recovery of the module intact. What is displaced is quarried limestone, in a surface application rather than a downcycled one.
No life-cycle assessment was carried out. These are qualitative potentials grounded in the protocol, not quantified claims.
Notes: The application envelope follows from the measurements rather than being imposed on them, and each condition traces to a specific result. Non-loadbearing surfaces, carrying self-weight and handling loads only, because 4.1 megapascals supports nothing more. Dry interiors, not wet rooms and not facades, because water performance depends on coating integrity. Away from ignition sources: it self-extinguishes, but it carries no classification. And modular rather than sheet, which matters because damage is then replaced one unit at a time rather than refinishing a surface. On end of life: every constituent including the shellac is biodegradable, and reversible fixing allows the module to be recovered intact. What is displaced is quarried limestone, in a surface application rather than a downcycled one. The caveat: no life-cycle assessment was carried out, so these are qualitative potentials grounded in the protocol and not quantified claims.

## Slide 26
Limitations
Three classes, each with a defined remedy
Measurement
No dispersion data — means of three specimens, individual values not retained
Compressive strain assumed from observation, not instrumented
Shrinkage unquantified, so bulk density is a lower bound
Process
Flexural series confounded — glycerol and solids concentration moved together
Kerfed section calculated as solid, so flexural modulus is a lower bound
Manual stirring; a single laboratory and a single operator
Untested
Durability — humidity, thermal cycling, UV, microbial attack, ageing
Reaction-to-fire classification beyond ignitability
Life-cycle assessment
Each limitation above corresponds to a defined next experiment, set out on the following slide.
Notes: The limitations, grouped in three classes rather than listed, because the grouping is itself informative. Measurement: no dispersion data, strain assumed rather than instrumented, shrinkage unquantified so density is a lower bound. Process: the flexural series is confounded, the kerfed section was calculated as solid, and stirring was manual in a single laboratory by a single operator. Untested: durability of any kind, reaction-to-fire classification beyond ignitability, and life-cycle assessment. I would rather set these out than have them found. Each one corresponds to a defined next experiment, which is the next slide.

## Slide 27
Further work
Four experiments, in order of what each one resolves
01
Repeat with dispersion reported
Three or more specimens per formulation with individual values retained, so that standard deviations and a coefficient of variation can be reported.
02
Record post-drying geometry
Measure and log the dried cross-section, converting every lower bound in this presentation into a true stress and a true density.
03
Instrument the strain
Replace the assumed 10% deformation with measured strain, yielding a real stress–strain curve and a defensible modulus of resilience.
04
Test an un-kerfed section
Separate the geometric contribution from the material contribution, so that the flexural modulus becomes a material constant.
Beyond these four: humidity and thermal cycling, microbial resistance, a reaction-to-fire classification, and a life-cycle assessment to support the environmental argument quantitatively.
Notes: Four experiments, in order of what each one resolves. First, repeat with individual specimen values retained so dispersion can be reported - that is the most commonly requested addition and the cheapest to supply. Second, record post-drying geometry, which converts every lower bound in this presentation into a true value. Third, instrument the strain, which replaces the assumed ten percent deformation with a measured curve and makes the modulus of resilience defensible rather than indicative. Fourth, test an un-kerfed section, which separates the geometric contribution from the material one. Beyond those four: humidity and thermal cycling, microbial resistance, a reaction-to-fire classification, and a life-cycle assessment.

## Slide 28
Conclusions
01
A protocol that can be repeated
every production parameter reported
02
Packing density governs compressive strength
not mineral content
03
Plasticiser content sets brittle or ductile response
the transition is sharp
04
Bio-polymer stiffness without thermal processing
water-cast, ambient-dried
05
Strength alone is an insufficient criterion
report σ and E together
Betül Ünal · b.unal91@gmail.com
Testing: Advanced Construction Materials Research Laboratory, Hacettepe University, with thanks to Dr Hüseyin İlcan. Derived from the author's doctoral dissertation, Hacettepe University, 2025.
Notes: Five conclusions. A protocol that can be repeated, reported parameter by parameter. Packing density, not mineral content, governs compressive strength. Plasticiser content sets a brittle or a ductile response, and the transition is sharp. A water-cast, ambient-dried material reaches bio-polymer stiffness without thermal processing. And strength alone is an insufficient criterion for this class: deformation capacity governs service behaviour, so strength and modulus should be reported together. Thank you. I am happy to take questions.

## Slide 29
References
Adogla, F., Yalley, P.P.K. & Arkoh, M. (2016) Improving compressed laterite bricks using powdered eggshells. The International Journal of Engineering and Science, 5(4), 65–70.
Altun, İ.A. (2006) Mechanical properties of travertine. Afyon Kocatepe University.
Arnaud, L. & Gourlay, E. (2012) Experimental study of parameters influencing mechanical properties of hemp concretes. Construction and Building Materials, 28(1), 50–56.
Ashby, M.F. (2011) Materials selection in mechanical design. 4th edn. Oxford: Butterworth-Heinemann.
ASTM International (2017) ASTM D790-17: Flexural properties of unreinforced and reinforced plastics. West Conshohocken, PA.
ASTM International (2018) ASTM D570-98: Water absorption of plastics. West Conshohocken, PA.
Bhartiya, A. & Dubey, M. (2018) Replacement of cement with coconut shell ash and egg shell powder. IRJET, 5(6).
Bilici, V.O., Peşmen, G., Yönetken, A. & Erol, A. (2023) Effect of egg-shell particulate reinforcement in ceramic-metal composites. Thermal Science, 27(4B), 3179–3188.
Faruk, O., Bledzki, A.K., Fink, H.-P. & Sain, M. (2012) Biocomposites reinforced with natural fibers. Progress in Polymer Science, 37(11), 1552–1596.
Hernández, V. et al. (2022) Agar biopolymer films for biodegradable packaging: a reference dataset. Materials, 15(11), 3954.
Hirschler, M.M. (2013) Flammability and fire testing. In: Handbook of environmental degradation of materials. Oxford: William Andrew, 197–230.
Holling, C.S. (1973) Resilience and stability of ecological systems. Annual Review of Ecology and Systematics, 4, 1–23.
International Organization for Standardization (2020) ISO 11925-2: Ignitability of products subjected to direct impingement of flame — single-flame source test. Geneva.
Islam, M.R., Tudryn, G., Bucinell, R., Schadler, L. & Picu, R.C. (2018) Mechanical behavior of mycelium-based particulate composites. Journal of Materials Science, 53, 16371–16382.
Jones, M., Mautner, A., Luenco, S., Bismarck, A. & John, S. (2020) Engineered mycelium composite construction materials. Journal of Bionanoscience, 14(1), 1–10.
Karana, E., Barati, B., Rognoli, V. & Zeeuw van der Laan, A. (2015) Material driven design (MDD). International Journal of Design, 9(2), 35–54.
Kim, H.-S. & Pal, K. (2010) Mechanical properties of eggshell-filled poly(lactic acid) composites. Macromolecular Research.
Klyosov, A.A. (2007) Wood-plastic composites. Hoboken, NJ: Wiley-Interscience.
Mansour, G., Zoumaki, M., Tsongas, K. & Tzetzis, D. (2021) Microstructural and finite element analysis of soy protein isolate bioplastics. Materials, 14(19), 5479.
Nemli, G. & Aydın, A. (2007) Evaluation of the physical and mechanical properties of particleboard. Building and Environment, 42(3), 1210–1214.
Owuamanam, S. & Cree, D. (2020) Progress of bio-calcium carbonate waste eggshell and seashell fillers in polymer composites: a review. Journal of Composites Science, 4(2), 70.
Pope, D.G. & Hudson, R.G. (1989) Mechanical properties of timber. Structural Engineer.
Razzaq, A.K. & Yousif, R.A. (2017) Sustainability of HMA by using of egg shell powder. International Conference on Sustainable Futures, Bahrain.
Shafiei, S. et al. (2019) Egg shell-derived calcium phosphate/carbon dot nanofibrous scaffolds. Materials Science and Engineering: C, 100, 564–575.
Shah, D.U., Vollrath, F., Stires, J. & Deheyn, D.D. (2016) Housing fly larvae in silk: mechanical properties of mineral-filled biocomposites. Materials & Design, 109, 723–731.
Skórczewska, K., Kwiatkowski, W. & Kwiatkowski, M. (2020) Poly(vinyl chloride) composites with waste eggshell as a natural filler. Polymer Composites, 41(9), 3580–3589.
Soundara, B. & Vilasini, P.P. (2015) Effect of egg shell powder on the properties of clay. 50th Indian Geotechnical Conference, Pune.
Teara, A. et al. (2019) Durability of fly ash and eggshell powder to replace cement in concrete. IOP Conf. Series: Earth and Environmental Science, 244, 012025.
Torres, F.G., Troncoso, O.P., Piaggio, F. & Hijar, A. (2010) Structure–property relationships of a biopolymer network: the eggshell membrane. Acta Biomaterialia, 6(9), 3687–3693.
Tutuş, A. et al. (2018) Evaluation of egg shells in wallpaper production. 1st International Technological Sciences and Design Symposium, Giresun.
Velasco, P.M. & Gaona, J.L. (2011) Mechanical characterisation of compressed agricultural-waste panels. Construction and Building Materials.
Victor, E.I., Louis, I.C., Alfred, N.O. & Ozioma, U.N. (2019) Use of chicken eggshells as fillers in flexible polyurethane foam. International Journal of Industrial Engineering, 3(1), 1–6.
Vilarinho, I.S., Filippi, E. & Seabra, M.P. (2022) Development of eco-ceramic wall tiles with bioCaCO₃ from eggshells waste. Open Ceramics, 9, 100220.
William, J.S. & Owen, J.C. (1995) Egg science and technology. 4th edn. Boca Raton, FL: CRC Press.
Yönetken, A., Erol, A., Yakar, A. & Peşmen, G. (2016) Ceramic-metal composites produced by electroless Ni plating of AlN-Astaloy Cr-M. IJCMNMME, 10(3).
Zhao, X. et al. (2022) Mechanical recycling of low-density polyethylene: property evolution. Resources, Conservation and Recycling.
Standards applied: ASTM D790-17 · ISO 11925-2:2020 · ASTM D570-98(2018).
Notes: References, left up for questions.