Photograph

Organization Logo

Title:

Eggshell–Agar Biocomposites for Interior Surfaces: A Production Protocol and Exploratory Characterisation

Author Name(s):

Betül Ünal

University/Organization:

Department of Interior Architecture, Cappadocia University, Nevşehir, Türkiye

Authors' Email ID(s):

b.unal91@gmail.com

Abstract:

Millions of tonnes of eggshell waste are generated each year, yet its valorisation in construction is dominated by use as a mineral filler in polymer or cement matrices whose binder remains petrochemical or clinker-based. This study reports a fully bio-based alternative: waste eggshell powder bound in an agar–glycerol matrix.

The principal contribution is a reproducible production protocol. Shells are heat-treated at 120 °C, milled, and sieved to 150 µm. Agar is dissolved in a water–glycerol phase at 95 °C, then held at 80 °C under continuous stirring for 55 minutes, with the mineral fraction added incrementally near the end. The mixture is cast in silicone moulds, dried four days at ambient temperature, and consolidated for seven days. This addresses a known barrier in designer-led biofabrication, where absent shared procedures prevent reproduction and comparison.

Characterisation covers compression, three-point flexure, ignitability, and water absorption, and is an exploratory baseline, not design values. Raising the mineral and agar fractions while reducing water increased compressive load capacity from 3.89 to 6.80 kN. Halving the glycerol content shifted the material from unmeasurably ductile to a flexural strength of 2.33 MPa at a modulus of 192 MPa. Specimens self-extinguished four seconds after flame removal; shellac-coated specimens absorbed 0.7% of their mass over 24 hours of immersion.

The low flexural modulus of such materials, conventionally reported as a deficiency, yields a modulus of resilience exceeding that of brittle mineral interior materials. The study therefore proposes resilience rather than strength as the governing evaluation criterion.

Keywords:

eggshell waste, biocomposite, biofabrication protocol, material resilience, circular design

Biography:

Betül Ünal is an Assistant Professor in the Department of Interior Architecture at Cappadocia University, Türkiye. She completed her PhD in 2025 at the Department of Interior Architecture and Environmental Design, Hacettepe University, with a dissertation on the production of biology-based materials and their analysis through spatial resilience. Her research addresses biodesign, material-driven design methods, the valorisation of organic waste streams, and the development of bio-based composites for interior applications. She has previously taught at the Faculty of Architecture and Design, Bahçeşehir University.